# MTRL 466 MEETING MINUTES

| Project Name: | Process Modelling for Adhesive Bonding of Aluminum Automotive Sheet |
| --- | --- |
| Group: | 1 |
| Current Meeting: | Friday, October 6, 2011 |
| Minutes Prepared By: | Adam Ohashi |

Attendees:

Dr. Chad Sinclair

GROUP 1: Jerry Chang, Michael Fu, Judy Makmillen, Adam Ohashi

Agenda:

- Gantt chart / timeline review:

  - On time for model development

  - May require more time for verification / tuning / sensitivity

  - Need to begin building the midterm presentation, midterm report ASAP

- Progress on development of models:

  - Heat transfer/thermal (Jerry/Mike)

    - Developed a working model for heat transfer for a basic Al-epoxy-Al configuration panel, printing out reasonable values based off placebo data

      - Adhesive layer contribution to heat transfer determined

      - 2 surface nodes, 5 internal nodes

      - Sensitivity testing underway; no determination of Δx value yet

      - Conductivity dependence on composition?

  - Recovery softening (Adam)

    - Developed a working model for characteristic yield stress softening during annealing of 5xxx, sensitivity tested

      - Model uses K coefficient, activation energy and activation volume as variable parameters

        - Activation volume is the key tuning variable

          - Relation between volume and temperature?

        - Uo is defined by activation energy Q in Al-Al diffusivity

      - Model based on Verdier equ. (7)

        - More “physical” relation to material softening

  - Precipitation hardening (Judy)

    - Developed an excel model for the precipitation strengthening of 6xxx

      - Good agreement with the given data (plot attached)

      - Have implemented additive (non-isothermal) Avrami equation and confirmed that it gives the same results for fraction precipitated

      - For presentation next week: what other verification should we produce, should we put generate data for process?

  - Adhesive/curing (Judy)

    - Developed a model for curing of adhesive, sensitivity tested

      - Using t0.90 at 180C to evaluate the sensitivity of the model to varying α0 and Δt

- Midterm presentation:

  - Delegate sections of presentation for midterm

    - Should include: introduction, literature review, objectives, needs & constraints, models used and why, validation, future work

Minutes:

Meeting start time:

Meeting end time:

Action Items:

- Next meeting: