# MTRL 466 MEETING MINUTES

| Project Name: | Process Modelling for Adhesive Bonding of Aluminum Automotive Sheet |
| --- | --- |
| Group: | 1 |
| Current Meeting: | Friday, September 9, 2011 |
| Minutes Prepared By: | Adam Ohashi |

Attendees:

Dr. Chad Sinclair

GROUP 1: Jerry Chang, Michael Fu, Judy Makmillen, Adam Ohashi

GROUP 2: Mandy Chen, Kyle Huang, Shauna Litke, Andy Wen

Agenda:

- Brief project review by Chad

  - Al alloys in automotive applications

  - Joining methods

  - Production logistics

  - Paint bake cycle

  - Description of empirical models

  - Validation methods

- Introduction to UBC Wiki

Minutes:

Meeting start time: 1:15pm

Meeting end time: 2:45pm

- Brief project review by Chad

  - Al alloys in automotive applications

    - Automotive side panels, components

    - 5xxx, 6xxx series

      - 5xxx series work hardened through deformation, non-heat treatable

      - 6xxx series precipitation hardening, heat treatable, aged

  - Joining methods

    - Combined via adhesive bonding, welding, mechanical fastening

    - Welding and mechanical fastening can induce corrosion (galvanic coupling, cracks), property changes, stress concentrations

    - Adhesion is corrosion resistant, convenient, minimal deterioration

  - Production logistics

    - Manufacturing assembly lines move quickly

    - Require the epoxy to cure quickly as well, around 200°C

  - Paint bake cycle

    - Dry powder application, around 150°C

  - Description of empirical models

    - Adhesive curing model

      - Coupling (heat source from oven air and epoxy reaction)

    - Heat transfer (thermal) model

    - Mechanical property model

      - Includes precipitation hardening and recovery softening

    - Should have models functional by midterm

  - Validation methods

    - Through literature and/or experimentation (time + resources)

    - Problem definition

    - Parameters, variables

  - Can we combine bonding, strengthening and paint bake process into 1 cycle?

    - Optimize the process based on time, performance, energy, cost

      - Feasibility, efficiency

- Introduction to UBC Wiki

  - Meeting minutes template

  - Introductory slides

  - Literature review papers

Action Items

- Divide tasks for group

  - Literature review

    - Review of Al alloys in automobiles, Al vs. steel

    - Al alloys common to automobile applications, composition, usage

    - Joining methods, focus on adhesive bonding, advantages vs. disadvantages

    - Paint bake cycle, methods

  - Model review

    - Adhesive curing

    - Heat transfer

    - Mechanical properties

- Create a schedule for coming weeks

  - Goals, expectations, deadlines

  - Model functionality by midterm

  - Set up a meeting with Goran to discuss epoxy bonding

- Every meeting requires a discussion leader and secretary

- Next meeting: Friday Sept. 16th, 12pm via Skype

  - Have agenda, progress report, meeting minutes ready

    - Uploaded to UBC Wiki