# MTRL 466 MEETING MINUTES

| Project Name: | Process Modelling for Adhesive Bonding of Aluminum Automotive Sheet |
| --- | --- |
| Group: | 1 |
| Current Meeting: | Friday, September 23, 2011 |
| Minutes Prepared By: | Adam Ohashi/Judy Makmillen |

Attendees:

Dr. Chad Sinclair

GROUP 1: Jerry Chang, Michael Fu, Judy Makmillen, Adam Ohashi

Agenda:

- Progress on literature reviews; have been revised after comments:

  - Review of Al alloys in automobiles (Jerry)

  - Al alloys common to automobile applications, composition, usage, vs. steel (Adam)

  - Joining methods, focus on adhesive bonding, advantages vs. disadvantages (Judy)

  - Paint bake cycle, methods (Mike)

- Progress on literature review and application of applicable models:

  - Heat transfer/thermal (Jerry/Mike)

    - Have spent some time searching for applicable information (parameters, boundary conditions, models) for heat transfer in Al alloys

      - Still pursuing valid resources

    - Intend to meet with Daan Maijer, Peter Barr to discuss heat transfer mechanics

  - Mechanical properties (Adam)

    - Familiar with Verdier’s recovery model; accessed his papers while working at Novelis

    - Continuing literature search, locating applicable papers

    - Judy has provided some literature based on precipitation hardening

  - Adhesive/curing (Judy)

    - Has a handle on the concepts of adhesive bonding

    - Progress on model: reviewed the paper uploaded by Chad onto the Wiki

    - Based on Goran's suggestion, should try and get a model working with those numbers and then work from there

      - Have an excel file started

    - Need an update on whether we are going to get more specific information from the manufacturer (after a model works we will need supplier specifications) or if we will just use the epoxy in the article

- Met with Goran Fernlund with Shauna from Group 2

Minutes:

Meeting start time: 1:40pm

Meeting end time: 3:00pm

- Literature review:

  - Government enforces CAFE Standards in the USA

    - Controls emissions

      - Penalties on emissions range globally

    - Intended to improve fuel economy in cars

  - Would be interesting to look into a social economic study of how Al alloys in automobiles affect the push for these standards

  - Can Al alloys replace steel in cars? ( Depends…

    - Type of loading

      - Materials selection charts, Ashby

        - Strength-to-density ratio, stiffness-to-density, strength-to-cost, etc…

    - Strength vs. stiffness; typically as strength increases, stiffness suffers

      - Less weight = less material = smaller cross-sectional area

- Models

  - Heat transfer:

    - Consider simple case; simple geometry (flat plate), fixed surface temperature, convection

      - Define temperature as a function of time and position

    - Need to understand differences in convective heat transfer vs. radiation heat transfer

  - Mechanical Properties:

    - Verdier paper (Recovery in Al-Mg alloys), equation (2), quasi-empirical model (phenomenological) = starting point for recovery model

    - Activation energy and activation volume are key variables

    - Given change in stress with time, temperature, calculate yield stress at given (T,t)

    - Precipitation model requires calculating macroscopic yield stress from microscopic stress changes

      - Need to also attribute solid solution stress contribution to overall stress evolution during precipitation hardening

  - Adhesion:

    - Model has been located, studied, tested by Judy

    - Need to consider experimental temperature testing range for validation of the model

      - Upper limit for temperature of epoxy curing?

    - No access to experimental validation for adhesives, use literature

  - All models:

    - Critical measurement: sensitivity testing

      - Validate initial conditions ( Do they make sense?

        - Play around with values at 0 time

        - Justify why these values are acceptable

    - Have all models be flexible

      - Should be able to adapt models to different heating processes, alloy types, epoxies, etc…

        - Have variable tuning parameters for easy manoeuvring

- Chad has contacted GM, Novelis

  - Specialists of adhesives, Al alloys

  - Chad can be the middleman; will communicate question we have to professionals

    - Questions must be valid, researched, tried but to no avail

      - Do not waste everyone’s time with meaningless/simple/unnecessary questions

Action Items:

- Chad to grant access to Ashby materials selection charts to Group 1

- Jerry and Mike to schedule meeting with Chad sometime on Monday, Sept. 26th to go over progress on heat transfer model

  - Jerry/Mike to review the basics of convective heat transfer, apply to simple geometry

- Have decoupled models working by next Friday’s meeting

  - Should have an Excel spreadsheet running with model

  - Continue literature review on models

- Next meeting: 12:00 pm (tentative) Friday, Sept. 30th