# MTRL 466 MEETING MINUTES

| Project Name: | Process Modelling for Adhesive Bonding of Aluminum Automotive Sheet |
| --- | --- |
| Group: | 1 |
| Current Meeting: | Friday, October 6, 2011 |
| Minutes Prepared By: | Adam Ohashi |

Attendees:

Dr. Chad Sinclair

GROUP 1: Jerry Chang, Michael Fu, Judy Makmillen, Adam Ohashi

Agenda:

- Gantt chart / timeline review:

  - On time for model development

  - May require more time for verification / tuning / sensitivity

  - Need to begin building the midterm presentation, midterm report ASAP

- Progress on development of models:

  - Heat transfer/thermal (Jerry/Mike)

    - Developed a working model for heat transfer for a basic Al-epoxy-Al configuration panel, printing out reasonable values based off placebo data

      - Adhesive layer contribution to heat transfer determined

      - 2 surface nodes, 5 internal nodes

      - Sensitivity testing underway; no determination of Δx value yet

      - Conductivity dependence on composition?

  - Recovery softening (Adam)

    - Developed a working model for characteristic yield stress softening during annealing of 5xxx, sensitivity tested

      - Model uses K coefficient, activation energy and activation volume as variable parameters

        - Activation volume is the key tuning variable

          - Relation between volume and temperature?

        - Uo is defined by activation energy Q in Al-Al diffusivity

      - Model based on Verdier equ. (7)

        - More “physical” relation to material softening

  - Precipitation hardening (Judy)

    - Developed an excel model for the precipitation strengthening of 6xxx

      - Good agreement with the given data (plot attached)

      - Have implemented additive (non-isothermal) Avrami equation and confirmed that it gives the same results for fraction precipitated

      - For presentation next week: what other verification should we produce, should we put generate data for process?

  - Adhesive/curing (Judy)

    - Developed a model for curing of adhesive, sensitivity tested

      - Using t0.90 at 180C to evaluate the sensitivity of the model to varying α0 and Δt

- Midterm presentation:

  - Delegate sections of presentation for midterm

    - Should include: introduction, literature review, objectives, needs & constraints, models used and why, validation, future work

Minutes:

Meeting start time: 1:10pm

Meeting end time: 3:00pm

- With group 2, went over the details for the project midterm report, as per the template provided by Ed

  - Needs: need statement, should explain why our customer requires the product of our project, gives rationale

    - Emissions restraints (impetus of gov’t) ( fuel economy ( lightweight vehicles ( Al vs. steel, processing efficiency

    - Usage of modeling = predict outcome/feasibility, save time/money/resources

    - Adhesion to replace welding, Al to Al

  - Constraints: require explanation/justification, hard vs. soft, differentiate from objectives

    - Alloy type, geometry, heating equipment

  - Problem specification: design requirements based on needs/constraints

    - Be specific! Only one page available

    - Free variables = temperature, fan speed, heating type (convection vs. conduction vs. radiation), heating orientation (1 side vs. both sides)

  - Technical review: literature review of paint bake cycle, Al alloys usage (5xxx & 6xxx), adhesive properties

  - Design options: explain design options (which model and why), process for selection, future enhancements/changes

    - Model = physical meaning, justify usage of each model

    - Show validation of each model, fit of data

    - Future work = couple all models, define how we can calculate efficiency

  - Team responsibilities: communication, delegation of tasks, Gantt chart/timeline

    - Can link to Wiki

- Discussed logistics of presentation

  - 10-12 slides, 15 maximum

  - Can be similar to report structure, requires more synthesis to extract key points

  - Have an interesting first slide to grab attention

    - No need for an overview slide

  - Put references on the slides where data/ideas appear, not on an end slide

- Review of progress on models:

  - Heat transfer (Mike/Jerry)

    - Al-epoxy-Al configuration

    - Require data from adhesion model for heat transfer data from epoxy

    - Require density, heat transfer coefficient, specific heat of epoxy

      - Can use literature, databases

  - Recovery (Adam)

    - Activation energy range = 120 kJ/mol to 170 kJ/mol

      - Can account for Al-Al and Mg-Al diffusion

    - Normalize the stress to account for the fully recrystallized yield stress

    - Find the pre-strain dependence on the model

    - Find data for lower temperature testing

      - Currently only have from 200C to 250C, need temperatures from 140C to 200C

  - Precipitation (Judy)

    - Confidence in Avrami equ. From 5% to 95%

      - Stress should realistically peak then diminish against time

  - Adhesive (Judy)

    - Adjust the adhesive model to provide a heat flux from the epoxy

Action Items:

- Have a report draft (can be point form) with main ideas wanting to be discussed by Wed. 12th

  - This should aid in organizing for the presentation

- Adam to create a Google Doc for point form ideas for report/presentation

  - Group members to add their own ideas

- Heat transfer model:

  - Confirm appropriate values for epoxy

  - Complete validation used to justify parameters/data for numerical model, compare Newtonian cooling

- Recovery model:

  - Find pre-strain dependence of model

  - Find data for lower temperature testing (140C)

  - Fix for stress normalization

- Precipitation:

  - Create a 5%-95% confidence interval for the Avrami equ. to account for stress drop

- Adhesive:

  - Provide the heat transfer model with heat transfer data for epoxy

- Next meeting: Chad would like to have a dry run of the midterm presentation on Wednesday, October 12th, 2011